Black ‘Economy’ Grade NR / SBR 70° shore WJ110

Our ‘Economy’ Grade Natural Rubber and Styrene Butadiene rubber blend is used where a cheaper quality material will suit. Such as in simple applications such as packing pieces, dust seals, protection pads etc. where the material is not coming under any duress.

## Our Sheeting can be supplied plain or with self-adhesive backed tape (SAB). Rubber Strip to bespoke sizes are available along with customised sheets/gaskets.

Thickness: 0.5mm to 50mm

Sheet Size: 1.4m wide x 10m rolls (1mm to 6mm), 5m rolls 8mm – 25mm and in 2m x 1m sheets 25,30,40 and 50mm.

Finish: Smooth finish (SS), Cloth finish (CC) is available at certain thickness’ see below

TECHNICAL DATA

| STOCK ROLL SIZES [M X M X MM] | SURFACE FINISH | WEIGHT [KG/M2] |
| --- | --- | --- |
| 1mm x 1400mm x 10m | SS CC | 1.50 |
| 1.5mm x 1400mm x 10m | SS CC | 2.25 |
| 2mm x 1400mm x 10m | SS CC | 3.00 |
| 3mm x 1400mm x 10m | SS CC | 4.50 |
| 4mm x 1400mm x 10m | SS | 6.00 |
| 5mm x 1400mm x 10m | SS | 7.50 |
| 6mm x 1400mm x 10m | SS | 9.00 |
| 8mm x 1400mm x 5m | SS | 12.00 |
| 10mm x 1400mm x 5m | SS | 15.00 |
| 12mm x 1400mm x 5m | SS | 18.00 |
| 15mm x 1400mm x 5m | SS | 22.50 |
| 20mmx 1400mm x 5m | SS | 30.00 |
| 25mm x 1400mm x 5m | SS | 37.50 |
| 25mm x 1m x 2m | SS | 37.50 |
| 30mm x 1m x 2m | SS | 45.00 |
| 40mm x 1m x 2m | SS | 60 |
| 50mm x 1m x 2m | SS | 75 |

# SPECIFICATIONS COMPOUND

| SPECIFICATIONS COMPOUND | VALUES [TYPICAL] |
| --- | --- |
| Colour | Black |
| Compound: | NR / SBR |
| Density [specific gravity | 1.6 |
| Hardness [Degree Shore A] | 70° ± 5 |
| Tensile strength [Kg/cm2 . Polymer] | 30 |
| Elongation at break | 200 |
| Minimum temperature | -20°C |
| Maximum temperature | +70°C |
| Compression Set (70°C for 22 hours) % | N/A |

| SPECIFICATIONS COMPOUND | VALUES [TYPICAL] |
| --- | --- |
| Compound: | NR / SBR |
| Density [specific gravity | 1.6 |
| Hardness [Degree Shore A] | 70° ± 5 |
| Tensile strength [Kg/cm2 . Polymer] | 30 |
| Elongation at break | 200 |
| Minimum temperature | -20°C |
| Maximum temperature | +70°C |
| Compression Set (70°C for 22 hours) % | N/A |

Metroseal Datasheet Disclaimer: All recommendations and information contained in this specification sheet are to the best of our knowledge correct. Since conditions of service are beyond our control, users must satisfy themselves that the products are suitable for intended use. No warranty is given or implied in respect of information or recommendations or that any use of products will infringe rights belonging to other parties. In any event or occurrence our liability is limited to the invoice value ofour goods delivered to you. We reserve the right to change product design and properties without notice.