Black 100% High Grade EPDM Rubber 60° shore WJ1456

Failure to select the correct materials or products can result in damage to plant and equipment and personal injury. In specific applications, where critical conditions exist, we suggest you contact us, and we will consider with you the most suitable material or product. However, information supplied by William Johnston & Company Limited is intended only as technical co-operation and as a guide to the various uses of different products. No warranty is given in respect of information or recommendations by William Johnston & Company Limited which are only given for guidance and without any guarantee. The customer must satisfy themselves on the suitability of the material or product for the intended purpose. The correct fitting of products particularly is the responsibility of the customer.

| PROPERTIES | TEST METHOD | VALUES FPS UNITS | TEST METHOD | VALUES METRIC UNITS |
| --- | --- | --- | --- | --- |
| SPECIFIC GRAVITY | ASTM D297 | 1.15 | DIN 53508 | 1.15 |
| HARDNESS | ASTM D2240 | 60 ± 5 SH A | DIN 53505 | 60 ± 5 SH A |
| TENSILE STRENGTH (MIN) | ASTM D412 | 1425 PSI | DIN 53504 | 100 KG/CM2 |
| ELONGATION AT BREAK (MIN) | ASTM D412 | 300% | DIN 53504 | 300% |
| COMPRESSION SET (70ºC/24 HRS/25% SET) (MAX) | ASTM D395 METHOD B | 30% | DIN 53517 | 30% |
| TEAR RESISTANCE (ANGULAR) MIN | ASTM D624 | 168 LBS/INCH | DIN 53515 | 30 KG/CM |
| CHANGE IN PROPERTIES |  |  |  |  |
| HEAT AGEING (72 HRS. AT 70ºC) | ASTM D573 |  |  |  |
| --- HARDNESS (PTS) |  | + 3 (MAX) |  | + 3 (MAX) |
| --- TENSILE STRENGTH (%) |  | + 10 / - 10 |  | + 10 / - 10 |
| --- ELONGATION AT BREAK (%) |  | + 10 / - 10 |  | + 10 / - 10 |
| VOLUME SWELL: AT 70ºC FOR 72 HRS/IN | ASTM D 471 |  |  |  |
| ASTM OIL NO.1 |  | NOT RECOMMENDED |  | NOT RECOMMENDED |
| ASTM OIL NO.2 |  | NOT RECOMMENDED |  | NOT RECOMMENDED |
| ASTM OIL NO.3 |  | NOT RECOMMENDED |  | NOT RECOMMENDED |
| POLYMER CONTENT (EPDM) |  | 100% |  | 100% |
| CHEMICAL RESISTANCE |  |  |  |  |
| --- OZONE | ASTM D 1149 | EXCELLENT |  | EXCELLENT |
| --- DILUTE ACIDS AND BASES |  | EXCELLENT |  | EXCELLENT |
| --- CONCENTRATED ACIDS AND BASES |  | EXCELLENT |  | EXCELLENT |
| --- OILS |  | NOT RECOMMENDED |  | NOT RECOMMENDED |
| --- SOLVENTS |  | NOT RECOMMENDED |  | NOT RECOMMENDED |
| TEMPERATURE RANGE |  | -30ºTO + 130ºC |  | -30ºTO + 130ºC |
| COLOUR |  | BLACK |  |  |