Black BS EN682 2002 Gas Grade Nitrile 70° shore (BS2494G) WJ2494

A specification grade of Nitrile suitable for elastomeric seals in pipes and fittings carrying gas and some hydrocarbon fluids.

| Properties | Values |
| --- | --- |
| Colour | Black |
| Compound | NBR |
| Density [Specific Gravity] | 1.20 |
| Hardness [Degrees Shore A] | 70˚ ± 5 |
| Tensile Strength [kg/cm2] | 100 |
| Elongation at Break | 200 |
| Minimum Temperature | -30˚C |
| Maximum Temperature | 120 ˚C |
| Polymer Content | 100% |
| Thickness | 1.5mm, 3.0mm, 4.5mm 6.0mm |
| Application | Seals for Gas and some Hydrocarbons |
| Finish | Cloth pattern both sides |

Failure to select the correct materials or products can result in damage to plant and equipment and personal injury. In specific applications, where critical conditions exist, we suggest you contact us, and we will consider with you the most suitable material or product. However, information supplied by William Johnston & Company Limited is intended only as technical co-operation and as a guide to the various uses of different products. No warranty is given in respect of information or recommendations by William Johnston & Company Limited which are only given for guidance and without any guarantee. The customer must satisfy themselves on the suitability of the material or product for the intended purpose. The correct fitting of products particularly is the responsibility of the customer.