Black Commercial Grade NR EPDM Rubber 65° Shore WJ117

| PROPERTIES | TEST METHOD | VALUES FPS UNITS | TEST METHOD | VALUES METRIC UNITS |
| --- | --- | --- | --- | --- |
| SPECIFIC GRAVITY | DIN 53508 | 1.35 ± 0.05 | ASTM D297 | 1.35 ± 0.05 |
| HARDNESS | DIN 53505 | 60 ± 5 SH A | ASTM D2240 | 60 ± 5 SH A |
| TENSILE STRENGTH (KG/CM2) | DIN 53504 | 711 PSI | ASTM D412 | 60 KG/CM2 |
| ELONGATION AT BREAK ( MIN ) | DIN 53504 | 300% | ASTM D412 | 300% |
| COMPRESSION SET (70ºC/24 HRS/25% SET) (MAX) | DIN 53517 | 35% | ASTM D395 METHOD B | 35% |
| TEAR RESISTANCE ( ANGULAR ) MIN | DIN 53515 | 101 LBS/INCH | ASTM D624 | 18 KG/CM |
| CHANGE IN PROPERTIES |  |  |  |  |
| HEAT AGEING (72 HRS. AT 70ºC) |  |  | ASTM D573 |  |
| --- HARDNESS (PTS) |  | + 3 (MAX) |  | + 3 (MAX) |
| --- TENSILE STRENGTH (%) |  | +10 / - 15 |  | +10 / - 15 |
| --- ELONGATION AT BREAK (%) |  | +10 / - 15 |  | +10 / - 15 |
| VOLUME SWELL: AT 70ºC FOR 72 HRS/IN |  |  | ASTM D 471 |  |
| IRM OIL NO.1 |  | NOT RECOMMENDED |  | NOT RECOMMENDED |
| IRM OIL NO.2 |  | NOT RECOMMENDED |  | NOT RECOMMENDED |
| IRM OIL NO.3 |  | NOT RECOMMENDED |  | NOT RECOMMENDED |
| POLYMER CONTENT (EPDM) |  | 30% |  | 30% |
| CHEMICAL RESISTANCE |  |  |  |  |
| --- OZONE |  | GOOD |  | GOOD |
| --- DILUTE ACIDS AND BASES |  | GOOD |  | GOOD |
| --- CONCENTRATED ACIDS AND BASES |  | FAIR |  | FAIR |
| --- OILS |  | NOT RECOMMENDED |  | NOT RECOMMENDED |
| --- SOLVENTS |  | NOT RECOMMENDED |  | NOT RECOMMENDED |
| TEMPERATURE RANGE |  | -30 º TO +100º C |  | -30 º TO +100º C |
| Colour |  | BLACK |  |  |

Failure to select the correct materials or products can result in damage to plant and equipment and personal injury. In specific applications, where critical conditions exist, we suggest you contact us, and we will consider with you the most suitable material or product. However, information supplied by William Johnston & Company Limited is intended only as technical co-operation and as a guide to the various uses of different products. No warranty is given in respect of information or recommendations by William Johnston & Company Limited which are only given for guidance and without any guarantee. The customer must satisfy themselves on the suitability of the material or product for the intended purpose. The correct fitting of products particularly is the responsibility of the customer.