Black Commercial Premium Quality 1 ply Insertion NR SBR 70° shore WJ126

| PROPERTIES | TEST METHOD | VALUES FPS UNITS | TEST METHOD | VALUES METRIC UNITS |
| --- | --- | --- | --- | --- |
| SPECIFIC GRAVITY | ASTM D297 | 1.5 | DIN 53508 | 1.5 |
| HARDNESS | ASTM D2240 | 70 ± 5 SH A | DIN 53505 | 70 ± 5 SH A |
| TENSILE STRENGTH (MIN) | ASTM D412 | 426 PSI | DIN 53504 | 30 KG/CM2 |
| ELONGATION AT BREAK (MIN) | ASTM D412 | 200% | DIN 53504 | 200% |
| TEAR RESISTANCE (ANGULAR) MIN | ASTM D624 | 90 LBS/INCH | DIN 53515 | 16 KG/CM |
| CHANGE IN PROPERTIES |  |  |  |  |
| HEAT AGEING (72 HRS. AT 70 ºC) | ASTM D573 |  |  |  |
| --- HARDNESS (PTS) |  | + 5 (MAX) |  | + 5 (MAX) |
| --- TENSILE STRENGTH (%) |  | + 10 / -25 |  | + 10 / -25 |
| --- ELONGATION AT BREAK (%) |  | + 10 / -25 |  | + 10 / -25 |
| VOLUME SWELL: AT 70ºC FOR 72 HRS/IN | ASTM D 471 |  |  |  |
| ASTM OIL NO.1 |  | NOT RECOMMENDED |  | NOT RECOMMENDED |
| ASTM OIL NO.2 |  | NOT RECOMMENDED |  | NOT RECOMMENDED |
| ASTM OIL NO.3 |  | NOT RECOMMENDED |  | NOT RECOMMENDED |
| CHEMICAL RESISTANCE |  |  |  |  |
| --- OZONE | ASTM D 1149 | NOT RECOMMENDED |  | NOT RECOMMENDED |
| --- DILUTE ACIDS AND BASES |  | NOT RECOMMENDED |  | NOT RECOMMENDED |
| --- CONCENTRATED ACIDS AND BASES |  | NOT RECOMMENDED |  | NOT RECOMMENDED |
| --- OILS |  | NOT RECOMMENDED |  | NOT RECOMMENDED |
| --- SOLVENTS |  | NOT RECOMMENDED |  | NOT RECOMMENDED |
| TEMPERATURE RANGE |  | -20º TO + 70º C |  | -20º TO + 70º C |
| COLOUR |  | BLACK |  | BLACK |
| APPREANCE |  | 1PLY COTTON 22+/-•?5 GSM FABRIC |  |  |

Metroseal, Units 28-30 Purdeys Way, Purdeys Industrial Estate, Rochford, Essex, SS4 1ND Phone: +44 (0) 1702 548800 | Fax: +44 (0)1702 549966 | Email: sales@metroseal.co.uk