Black Diamond Drum Lagging – Mini Diamond WJ218

| PROPERTIES | TEST METHOD | VALUES FPS UNITS | TEST METHOD | VALUES METRIC UNITS |
| --- | --- | --- | --- | --- |
| SPECIFIC GRAVITY | ASTM D297 | 1.17 | DIN 53508 | 1.17 |
| HARDNESS | ASTM D2240 | 65 ± 5 SH A | DIN 53505 | 65 ± 5 SH A |
| TENSILE STRENGTH (MIN) | ASTM D412 | 1638 PSI | DIN 53504 | 115 KG/CM2 |
| ELONGATION AT BREAK (MIN) | ASTM D412 | 450% | DIN 53504 | 450% |
| ABRASION RESISTANCE (MAX) | ASTM D5963 | 120 MM3 | DIN 53516 | 120 MM3 |
| COMPRESSION SET (70 ºC/24 HRS/25% SET) (MAX) | ASTM D395 METHOD B | 30% | DIN 53517 | 30% |
| TEAR RESISTANCE (ANGULAR) MIN | ASTM D624 | 168 LBS/INCH | DIN 53515 | 30 KG/CM |
| CHANGE IN PROPERTIES |  |  |  |  |
| HEAT AGEING (72 HRS. AT 70 ºC) | ASTM D573 |  |  |  |
| --- HARDNESS (PTS) |  | + 5 (MAX) |  | + 5 (MAX) |
| --- TENSILE STRENGTH (%) |  | + 10 / - 25 |  | + 10 / - 25 |
| --- ELONGATION AT BREAK (%) |  | + 10 / - 25 |  | + 10 / - 25 |
| VOLUME SWELL: AT 70ºC FOR 72 HRS/IN | ASTM D 471 |  |  |  |
| ASTM OIL NO.1 |  | NOT RECOMMENDED |  | NOT RECOMMENDED |
| ASTM OIL NO.2 |  | NOT RECOMMENDED |  | NOT RECOMMENDED |
| ASTM OIL NO.3 |  | NOT RECOMMENDED |  | NOT RECOMMENDED |
| CHEMICAL RESISTANCE |  |  |  |  |
| --- OZONE | ASTM D 1149 | FAIR |  | FAIR |
| --- DILUTE ACIDS AND BASES |  | GOOD |  | GOOD |
| --- CONCENTRATED ACIDS AND BASES |  | NOT RECOMMENDED |  | NOT RECOMMENDED |
| --- OILS |  | NOT RECOMMENDED |  | NOT RECOMMENDED |
| --- SOLVENTS |  | NOT RECOMMENDED |  | NOT RECOMMENDED |
| TEMPERATURE RANGE |  | -30º TO + 70ºC |  | -30º TO + 70ºC |

| PROPERTIES | TEST METHOD | VALUES FPS UNITS | TEST METHOD | VALUES METRIC UNITS |
| --- | --- | --- | --- | --- |
| COLOUR & DESIGN |  | BLACK /RED /BLUE WITH GREY NEOPRENE BONDING LAYER & DIAMOND DESIGN |  |  |