Black EPDM Roofing Membrane Sheeting WJ146

Failure to select the correct materials or products can result in damage to plant and equipment and personal injury. In specific applications, where critical conditions exist, we suggest you contact us, and we will consider with you the most suitable material or product. However, information supplied by William Johnston & Company Limited is intended only as technical co-operation and as a guide to the various uses of different products. No warranty is given in respect of information or recommendations by William Johnston & Company Limited which are only given for guidance and without any guarantee. The customer must satisfy themselves on the suitability of the material or product for the intended purpose. The correct fitting of products particularly is the responsibility of the customer.

| PROPERTIES | TEST METHOD | VALUES FPS UNITS | TEST METHOD | VALUES METRIC UNITS |
| --- | --- | --- | --- | --- |
| COLOUR | VISUAL | BLACK |  | BLACK |
| DENSITY |  | 1.10 |  | 1.10 |
| HARDNESS | ASTM D 2240 | 65 ± 10 SH A | DIN 53505 | 65 ± 10 SH A |
| TENSILE STRENGTH ( MIN ) | ASTM D 412 | 90KG/CM | DIN 53504 | 1280.7 PSI |
| ELONGATION AT BREAK ( MIN ) | ASTM D 412 | 300% | DIN 53504 | 300% |
| ABRASION RESISTANCE ( MAX ) | ASTM D5963 | 250 MM | DIN 150 4649 | 250 MM |
| POLYMER CONTENT (%) |  | 100 |  | 100 |
| COMPRESSION SET (70 C/24 HRS) \(MAX) | ASTM D395 METHOD B | 24% | DIN 180 815 | 24% |
| TEAR RESISTANCE (ANGULAR) MIN | ASTM D624 METHOD C | 30 KG/CM | DIN 53506 | 167.97 LBS/INCH |
| RESISTANCE TO HEAT AGING |  |  |  |  |
| PROPERTIES AFTER 166 HRS @ 115C | ASTM D 573 |  |  |  |
| TENSILE STRENGTH MIN. | ASTM D 412 | 85KGS. /CM2 | DIN 53505 | 1209.55 PSI |
| ELONGATION ( % ) | ASTM D 412 | 210 | DIN 53504 | 210 |
| LINEAR DIMENSIONAL CHANGE MAX. % | ASTM D 1204 | +/-1 |  |  |
| BRITTLENESS TEMPERATURE C | ASTM D 746 | -45 |  |  |
| RESISTANCE WATER ABSORPTION, AFTER 166HRS. ° IMMERSION @ 70 C |  |  |  |  |
| % CHANGE IN MASS | ASTM D 471 | 4.0 | DIN ISO 1817 | 4.0 |
| WATER VAPOR PERMEABILITY MAX. PER- MILLS | ASTM E 96 | 3.5 |  |  |
| TEMPERATURE RESISTANCE |  | -30 TO +120°C |  |  |