Black Economy 1 ply insertion NR SBR Rubber 70° shore WJ120

Our Black Commercial quality 1 ply insertion NR / SBR 70° is an ‘Economy’ Grade Natural Rubber and Styrene Butadiene rubber blend. It is used where a cheaper quality material will suit. Such as in simple applications such as packing pieces, dust seals, protection pads etc. where the material is not coming under any duress.

Our Sheeting can be supplied plain or with self-adhesive backed tape (SAB). Rubber Strip to bespoke sizes are available along with customised sheets/gaskets.

Material Profile: See below Thickness: 0.5mm to 50mm

Sheet Size: 1.4m wide in 5, 10 and 20m rolls

Finish: Smooth (SS)

TECHNICAL DATA

| STOCK ROLL SIZES [M X M X MM] | SURFACE FINISH | WEIGHT [KG/M2] |
| --- | --- | --- |
| 1.5mm x 1400mm x 10m |  | 240 |

| 2mm x 1400mm x 10m |  | 3.20 |
| --- | --- | --- |
| 2.5mm x 1400mm x 10m |  | 400 |
| 3mm x 1400mm x 10m |  | 4.80 |
| 4mm x 1400mm x 10m |  | 6.40 |
| 5mm x 1400mm x 10m |  | 8,00 |
| 6mm x 1400mm x 10m |  | 9.60 |
| 8mm x 1400mm x 5m |  | 12.80 |
| 10mm x 1400mm x 5m |  | 16.00 |
| 12mm x 1400mm x 5m |  | 18.20 |

# SPECIFICATIONS COMPOUND

| SPECIFICATIONS COMPOUND | VALUES [TYPICAL] |
| --- | --- |
| Colour | Black |
| Compound | NR/SBR |
| Density (S.G.) | 1.6 |
| Hardness Shore 'A' (±5) | 70° ± 5° |
| Tensile Strength (Kg/cm2) | 30 |
| Elongation at break (%) | 200 |
| Minimum Temperature | -20°C |

| Maximum temperature | +70°C |
| --- | --- |
| Abrasion resistance (mm?) | NA |