Black Fuel Resistant Nitrile/PVC 65° shore WJ175

| PROPERTIES | TEST METHOD | VALUES FPS UNITS | TEST METHOD | VALUES METRIC UNITS |
| --- | --- | --- | --- | --- |
| SPECIFIC GRAVITY | ASTM D297 | 1.25 | DIN 53508 | 1.25 |
| HARDNESS | ASTM D2240 | 65 ± 5 SH A | DIN 53505 | 65 ± 5 SH A |
| TENSILE STRENGTH (MIN) | ASTM D412 | 995 PSI | DIN 53504 | 60 KG/CM2 |
| ELONGATION AT BREAK (MIN) | ASTM D412 | 250% | DIN 53504 | 250% |
| COMPRESSION SET (70ºC/24 HRS/25% SET) (MAX) | ASTM D395 METHOD B | 35% | DIN 53517 | 35% |
| ABRASION LOSS (MAX) | ASTM D 5963 | 300 MM3 | DIN 53516 | 300 MM3 |
| TEAR RESISTANCE (ANGULAR) MIN | ASTM D624 | 123 LBS/INCH | DIN 53515 | 22 KG/CM |
| CHANGE IN PROPERTIES |  |  |  |  |
| HEAT AGEING (72 HRS. AT 70ºC) | ASTM D 573 |  |  |  |
| --- HARDNESS (PTS) |  | + 6 (MAX) |  | + 6 (MAX) |
| --- TENSILE STRENGTH (%) |  | + 10 / -10 |  | + 10 / -10 |
| --- ELONGATION AT BREAK (%) |  | + 10 / -20 |  | + 10 / -20 |
| VOLUME SWELL: AT 70ºC FOR 72 HRS/IN | ASTM D 471 |  |  |  |
| ASTM OIL NO.1 |  | -2% |  | -2% |
| ASTM OIL NO.2 |  | + 4% |  | + 4% |
| ASTM OIL NO.3 |  | + 13% |  | + 13% |
| AT FUEL B /24 HRS/ROOM TEMP, MAX |  | + 25 % |  | + 25 % |
| POLYMER CONTENT (NITRILE/PVC BLEND) |  | BLEND |  | BLEND |
| CHEMICAL RESISTANCE |  |  |  |  |
| --- OZONE | ASTM D 1149 | GOOD |  | GOOD |
| --- DILUTE ACIDS AND BASES |  | GOOD |  | GOOD |
| --- CONCENTRATED ACIDS AND BASES |  | NOT RECOMMENDED |  | NOT RECOMMENDED |
| --- OILS |  | EXCELLENT |  | EXCELLENT |