Black NBR Nitrile Coated Nylon Diaphragm Sheeting 70 Shore to BS2751 BA70 – 0.40mm WJ195CO

| Properties |  | Test Method | Values FPS Units |
| --- | --- | --- | --- |
| Volume Swell: At 40ºC for 24hrs/in |  |  |  |
| Fuel B (Max) |  | BS 903: Part A16 | +25% |
| Resistance to low temperature in ºC at which the stiffness shall not exceed 70MPA |  | BS903: Part A13 | -25 |
| Adhesion to and corrosion of metals at 70ºC/168 hrs |  | BS 903: Part A37 | MEETS REQUIREMENTS |
| Polymer Content (Nitrile) |  |  | 100% |
| Additional Information |  |  |  |
| Chemical Resistance |  |  |  |
| Ozone |  | BS 903: Part A43 | FAIR |
| Dilute Acids and Bases |  | BS 903: Pat A16 | GOOD |
| Concentrated Acids and Bases |  |  | NOT RECOMMENDED |
| Mineral Oil/Petroleum |  |  | EXCELLENT |
| Solvents |  |  | FAIR |
| LPG/CNG |  |  | GOOD |
| Water |  |  | GOOD |
| Volume Swell: At 70ºC for 72 hrs/in |  |  |  |
| IRM / ASTM Oil No. 1 | - 3% |  |  |
| IRM / ASTM Oil No. 2 | - 2% |  |  |
| IRM / ASTM Oil No. 3 | + 10% |  |  |

| Nitrile Rubber Coated Fabric in Black for Diaphragm Sheet – 0.40mm |  |  |  |
| --- | --- | --- | --- |
| Elastomer Characteristics |  | Value | Test Method |
| Elastomer |  | NBR Nitrile Rubber | BS2751 BA70 |
| Hardness |  | 70 ± 5 SH A | DIN 53505 |
| Colour |  | Black |  |
| Fabric Characteristics |  |  |  |
| Fabric |  | 10054 |  |
| Weight |  | 105 GSM |  |
| Thickness |  | 0.17mm |  |
| Coated Fabric Characteristics |  |  |  |
| Thickness |  | 0.40 ± 0.05 |  |
| Weight |  | 500 ± 50 | ASTM D-751 IS-7016 (Pt-I) |
| Tensile Strength kg/50mm | Warp | 130 (min) | ASTM D-751 IS 7016-Part II ISO-1421 |
|  | Weft | 130 (min) |  |
| Elongation at Break | Warp | 30% (max) |  |
|  | Weft | 30% (max) |  |
| Adhesion (Peel Strength) kg/25mm |  | 5kg | ASTM D-751 |
| Temperature range |  | -25º to +110ºC |  |

Failure to select the correct materials or products can result in damage to plant and equipment and personal injury. In specific applications, where critical conditions exist, we suggest you contact us, and we will consider with you the most suitable material or product. However, information supplied by William Johnston & Company Limited is intended only as technical co-operation and as a guide to the various uses of different products. No warranty is given in respect of information or recommendations by William Johnston & Company Limited which are only given for guidance and without any guarantee. The customer must satisfy themselves on the suitability of the material or product for the intended purpose. The correct fitting of products particularly is the responsibility of the customer.