Black NBR Nitrile Coated Nylon Diaphragm Sheeting 70 Shore to BS2751 BA70 – 0.50mm WJ195CO

| Properties |  | Test Method | Values FPS Units |
| --- | --- | --- | --- |
| Volume Swell: At 40ºC for 24hrs/in |  |  |  |
| Fuel B (Max) |  | BS 903: Part A16 | +25% |
| Resistance to low temperature in ºC at which the stiffness shall not exceed 70MPA |  | BS903: Part A13 | -25 |
| Adhesion to and corrosion of metals at 70ºC/168 hrs |  | BS 903: Part A37 | MEETS REQUIREMENTS |
| Polymer Content (Nitrile) |  |  | 100% |
| Additional Information |  |  |  |
| Chemical Resistance |  |  |  |
| Ozone |  | BS 903: Part A43 | FAIR |
| Dilute Acids and Bases |  | BS 903: Pat A16 | GOOD |
| Concentrated Acids and Bases |  |  | NOT RECOMMENDED |
| Mineral Oil/Petroleum |  |  | EXCELLENT |
| Solvents |  |  | FAIR |
| LPG/CNG |  |  | GOOD |
| Water |  |  | GOOD |
| Volume Swell: At 70ºC for 72 hrs/in |  |  |  |
| IRM / ASTM Oil No. 1 | - 3% |  |  |
| IRM / ASTM Oil No. 2 | - 2% |  |  |
| IRM / ASTM Oil No. 3 | + 10% |  |  |

| Nitrile Rubber Coated Fabric in Black for Diaphragm Sheet – 0.50mm |  |  |  |
| --- | --- | --- | --- |
| Elastomer Characteristics |  | Value | Test Method |
| Elastomer |  | NBR Nitrile Rubber | BS2751 BA70 |
| Hardness |  | 70 ± 5 SH A | DIN 53505 |
| Colour |  | Black |  |
| Fabric Characteristics |  |  |  |
| Fabric |  | 10056 |  |
| Weight |  | 180 GSM |  |
| Thickness |  | 0.23mm |  |
| Coated Fabric Characteristics |  |  |  |
| Thickness |  | 0.50 ± 0.05 |  |
| Weight |  | 650 ± 50 | ASTM D-751 IS-7016 (Pt-I) |
| Tensile Strength kg/50mm | Warp | 175 (min) | ASTM D-751 IS 7016-Part II ISO-1421 |
|  | Weft | 175 (min) |  |
| Elongation at Break | Warp | 30% (max) |  |
|  | Weft | 30% (max) |  |
| Adhesion (Peel Strength) kg/25mm |  | 5kg | ASTM D-751 |
| Temperature range |  | -25º to +110ºC |  |