Black Natural Rubber to BS5400 Pt 9 Bridge Bearing WJ240

| PROPERTIES | TEST METHOD | VALUES FPS UNITS | TEST METHOD | VALUES METRIC UNITS |
| --- | --- | --- | --- | --- |
| SPECIFIC GRAVITY | BS 903: PART A1(Z) | 1.20 |  |  |
| HARDNESS | BS 903: PART A26 | 60 ± 5 IRHD |  |  |
| TENSILE STRENGTH (MIN) | BS 903: PART A2 | 155 KG/CM2 |  |  |
| ELONGATION AT BREAK (MIN) | BS 903: PART A2 | 400% |  |  |
| COMPRESSION SET (70ºC/24 HRS/25% SET) (MAX) | BS 903: PART A6 | 30% |  |  |
| TEAR RESISTANCE (ANGULAR) MIN | BS 903: PART A3 (Z) | 40 KG/CM |  |  |
| CHANGE IN PROPERTIES |  |  |  |  |
| HEAT AGEING (7 DAYS / 70ºC) | BS 903: PART A 19 |  |  |  |
| --- HARDNESS (PTS) | BS 903: PART A26 | + 10 / -10 (MAX) |  |  |
| --- TENSILE STRENGTH (%) | BS 903: PART A2 | -15 /+ 15 (MAX) |  |  |
| --- ELONGATION AT BREAK (%) | BS 903: PART A2 | - 20 / + 20 (MAX) |  |  |
| LOW TEMPERATURE BRITTLENESS | BS 903: PART A25 | BELOW -25ºC |  |  |
| LOW TEMPERATURE STIFFENING, (-25ºC/24 HRS), IRHD | BS 903: PART A26 | -0 / +15 IRHD(MAX) |  |  |
| "LOW TEMPERATURE CRYSTALLIZATION COMPRESSION SET @ -10ºC/10 DAYS" | BS 903: PART A39 | 65% (MAX) |  |  |
| "LOW TEMPERATURE CRYSTALLIZATION COMPRESSION SET @ -25ºC/3 DAYS" | BS 903: PART A39 | 65% (MAX) |  |  |
| SHEAR MODULUS (AT A STRAIN OF 0.25) | BS 903: PART A 14 | PASS |  |  |
| --- OZONE@25 PPHM/30ºC/96 HRS/20% STRETCH | BS 903: PART A 43 | NO VISIBLE CRACKS |  |  |

| PROPERTIES | TEST METHOD | VALUES FPS UNITS | TEST METHOD | VALUES METRIC UNITS |
| --- | --- | --- | --- | --- |
| POLYMER CONTENT (NATURAL RUBBER) |  | 100% |  |  |
| ADDITIONAL INFORMATION - |  |  |  |  |
| CHEMICAL RESISTANCE |  |  |  |  |
| --- DILUTE ACIDS AND BASES |  | NOT RECOMMENDED |  |  |
| --- CONCENTRATED ACIDS AND BASES |  | NOT RECOMMENDED |  |  |
| --- OILS |  | NOT RECOMMENDED |  |  |
| --- SOLVENTS |  | NOT RECOMMENDED |  |  |
| TEMPERATURE RANGE |  | -40º TO + 70ºC |  |  |
| COLOUR |  | BLACK |  |  |

Failure to select the correct materials or products can result in damage to plant and equipment and personal injury. In specific applications, where critical conditions exist, we suggest you contact us, and we will consider with you the most suitable material or product. However, information supplied by William Johnston & Company Limited is intended only as technical co-operation and as a guide to the various uses of different products. No warranty is given in respect of information or recommendations by William Johnston & Company Limited which are only given for guidance and without any guarantee. The customer must satisfy themselves on the suitability of the material or product for the intended purpose. The correct fitting of products particularly is the responsibility of the customer.