Black Neoprene Flame Retardant Sheet 60° shore WJ187

| Characteristics |  | Values |
| --- | --- | --- |
| Specific Gravity |  | 1.20 |
| Hardness (o Shore A) |  | 60 ± 5 |
| Tensile Strength, (Kgf/cm2), min |  | 80 |
| Elongation At Break, (%), min |  | 250 |
| Maximum compression set after 24h at 70oC, (%) |  | 25 |
| Flame resistance (according to ISO240) | Flame persistence (after removing the burner) | Max 45s |
|  | The flame mustn’t reappear after an air draughtiness application | Max 15 |
| Antistatic characteristic (according to BS 490) Surface electrical resistance (Ω), max |  | 3 x 108 |
| Temperature Range |  | -30o to +100oC |
| Compression Set (70oC for 22 hours), (%) |  | 25 |
| Polymer Content |  | Blend |