Black Neoprene Reinforced Sheeting to BS2752 C60 WJ196CT

| PROPERTIES | TEST METHOD | VALUES |
| --- | --- | --- |
|  |  | METRIC UNITS |
| SPECIFIC GRAVITY | BS 903: PART A1 | 1.40 |
| HARDNESS | BS 903: PART A26 | 60 ± 5 IRHD |
| TENSILE STRENGTH (KG/CM2) | BS 903: PART A2 | 130 |
| ELONGATION AT BREAK (MIN) | BS 903: PART A2 | 350% |
| COMPRESSION SET (70ºC/24 HRS/25% SET) (MAX) | BS 903: PART A6 | 25% |
| TEAR RESISTANCE (ANGULAR) MIN | BS 903: PART A3 | 35 Kg/cm |
| RESISTANCE TO ACCELERATED AGEING- 168HRS AT 70˚C | BS 903: PART A19 |  |
| --- HARDNESS (Pts) | BS 903: PART A26 | + 7 (MAX) |
| --- TENSILE STRENGTH (%) | BS 903: PART A2 | -12 (MAX) |
| --- ELONGATION AT BREAK (%) | BS 903: PART A2 | -20 (MAX) |
| VOLUME SWELL: AT 40˚C FOR 24 HRS/IN | BS 903: PART A16 |  |
| FUEL B |  | + 70% (MAX) |
| RESISTANCE TO LOW TEMPERATURE AT - 40ºC | BS 903: PART A13 | MEETS REQUIREMENTS |
| ADHESION TO AND CORROSION OF METALS | BS 903: PART A 37 | MEETS REQUIREMENTS |
| POLYMER CONTENT (NEOPRENE) |  | 100% |
| ADDITIONAL INFORMATION - |  |  |
| CHEMICAL RESISTANCE |  |  |
| --- OZONE | BS 903: PART A 43 | GOOD |
| --- DILUTE ACIDS AND BASES | BS 903: PART A16 | GOOD |
| --- CONCENTRATED ACIDS AND BASES |  | NOT RECOMMENDED |
| --- MINERAL OILS - PARAFINNIC & NAPHTHANIC HC |  | GOOD |
| --- MINERAL OILS - AROMATIC HC |  | FAIR |
| --ANIMAL/VEGETABLE OIL |  | GOOD |
| --SOLVENTS |  | FAIR |
| TEMPERATURE RANGE |  | -30º TO + 120º C |
| COLOUR | BLACK |  |
| FABRIC | 1PLY 150GSM Nylon fabric reinforcement |  |

| VOLUME SWELL DATA |  |  |
| --- | --- | --- |
| RESISTANCE TO LIQUIDS | BS ISO 1817, 24 0 h at (40±1) °C −2 | -0 |
| VOLUME CHANGE (%) AFTER IMMERSION IN LIQUID B | BS ISO 1817, 24 0 h at (40±1) °C −2 | +70 |
| RESISTANCE TO ACCELERATED AGEING | PART A19, AIR-OVEN METHOD A, (168±2) h, (70±1) °C | -0 |
| CHANGE IN HARDNESS DEGREES (IRHD) | PART A26, METHOD N, MEASUREMENTS BEFORE AND AFTER AGEING ON THE SAME 2 PLIES EACH 2.00MM THICK | +7 |
| MAXIMUM CHANGE IN TENSILE STRENGTH (% OF ORIGINAL VALUE) | PART A2, TYPE 1 OR TYPE 2 DUMBBELLS | -12 |
| MAXIMUM CHANGE IN ELONGATION AT BREAK (% OF ORIGINAL VALUE) | PART A2, TYPE 1 OR TYPE 2 DUMBBELLS | -20 |

Failure to select the correct materials or products can result in damage to plant and equipment and personal injury. In specific applications, where critical conditions exist, we suggest you contact us, and we will consider with you the most suitable material or product. However, information supplied by William Johnston & Company Limited is intended only as technical co-operation and as a guide to the various uses of different products. No warranty is given in respect of information or recommendations by William Johnston & Company Limited which are only given for guidance and without any guarantee. The customer must satisfy themselves on the suitability of the material or product for the intended purpose. The correct fitting of products particularly is the responsibility of the customer.