Black Neoprene to BS2752 C50 WJ180

| PROPERTIES | TEST METHOD | VALUES |
| --- | --- | --- |
|  |  | METRIC UNITS |
| SPECIFIC GRAVITY | BS 903: PART A1 | 1.35 |
| HARDNESS | BS 903: PART A26 | 50 ± 5 IRHD |
| TENSILE STRENGTH (KG/CM2) | BS 903: PART A2 | 90 |
| ELONGATION AT BREAK (MIN) | BS 903: PART A2 | 400% |
| COMPRESSION SET (70ºC/24 HRS/25% SET) (MAX) | BS 903: PART A6 | 30% |
| TEAR RESISTANCE (ANGULAR) MIN | BS 903: PART A3 | 30 Kg/cm |
| RESISTANCE TO ACCELERATED AGEING- 168HRS AT 70˚C | BS 903: PART A19 |  |
| --- HARDNESS (Pts) | BS 903: PART A26 | + 7 (MAX) |
| --- TENSILE STRENGTH (%) | BS 903: PART A2 | -12 (MAX) |
| --- ELONGATION AT BREAK (%) | BS 903: PART A2 | -20 (MAX) |
| VOLUME SWELL: AT 40˚C FOR 24 HRS/IN | BS 903: PART A16 |  |
| FUEL B |  | + 80% (MAX) |
| RESISTANCE TO LOW TEMPERATURE AT - 40ºC | BS 903: PART A13 | MEETS REQUIREMENTS |
| ADHESION TO AND CORROSION OF METALS | BS 903: PART A 37 | MEETS REQUIREMENTS |
| POLYMER CONTENT (NEOPRENE) |  | 100% |
| ADDITIONAL INFORMATION - |  |  |
| CHEMICAL RESISTANCE |  |  |
| --- OZONE | BS 903: PART A 43 | GOOD |
| --- DILUTE ACIDS AND BASES | BS 903: PART A16 | GOOD |
| --- CONCENTRATED ACIDS AND BASES |  | NOT RECOMMENDED |
| --- MINERAL OILS - PARAFINNIC & NAPHTHANIC HC |  | GOOD |
| --- MINERAL OILS - AROMATIC HC |  | FAIR |
| --ANIMAL/VEGETABLE OIL |  | GOOD |
| --SOLVENTS |  | FAIR |
| TEMPERATURE RANGE |  | -30º TO + 120º C |
| COLOUR | BLACK |  |

| VOLUME SWELL DATA |  |  |
| --- | --- | --- |
| RESISTANCE TO LIQUIDS | BS ISO 1817, 24 0-2h at (40±1) °C | -0 |
| VOLUME CHANGE (%) AFTER IMMERSION IN LIQUID B | BS ISO 1817, 24 0-2h at (40±1) °C | +80 |
| RESISTANCE TO ACCELERATED AGEING | PART A19, AIR-OVEN METHOD A, (168±2) h, (70±1) °C | -0 |
| CHANGE IN HARDNESS DEGREES (IRHD) | PART A26, METHOD N, MEASUREMENTS BEFORE AND AFTER AGEING ON THE SAME 2 PLIES EACH 2.00MM THICK | +7 |
| MAXIMUM CHANGE IN TENSILE STRENGTH (% OF ORIGINAL VALUE) | PART A2, TYPE 1 OR TYPE 2 DUMBBELLS | -12 |
| MAXIMUM CHANGE IN ELONGATION AT BREAK (% OF ORIGINAL VALUE) | PART A2, TYPE 1 OR TYPE 2 DUMBBELLS | -20 |