Black Nitrile to BS2751 BA50 WJ190

| PROPERTIES | TEST METHOD | VALUES |
| --- | --- | --- |
|  |  | METRIC UNITS |
| DENSITY (Mg/m3) | BS 903: PART A1 | 1.15 ± 0.02 |
| HARDNESS | BS903: PART A26 | 50 (+5-4) IRHD |
| TENSILE STRENGTH (MIN) | BS 903: PART A2 | 7.5 Mpa |
| ELONGATION AT BREAK (MIN) | BS 903: PART A2 | 450% |
| COMPRESSION SET (70ºC/24 HRS/25% SET) (MAX) | BS 903: PART A6 | 25% |
| TEAR RESISTANCE (ANGULAR) MIN | BS 903: PART A3 (Z) | 35 Kg/cm |
| RESISTANCE TO ACCELERATED AGEING – 168 HRS AT 70˚C | BS 903: PART A19 |  |
| --- HARDNESS (Pts) | BS 903: PART A26 | + 10 (MAX) |
| --- TENSILE STRENGTH (%) | BS 903: PART A2 | -10 (MAX) |
| --- ELONGATION AT BREAK (%) | BS 903: PART A2 | -35 (MAX) |
| VOLUME SWELL: AT 40˚C FOR 24 HRS/IN | BS 903: PART A16 |  |
| FUEL B |  | +30 (MAX) |
| RESISTANCE TO LOW TEMPERATURE IN ºC AT WHICH THE STIFNESS SHALL NOT EXCEED 70 MPA | BS 903: PART A13 | -30 |
| ADHESION TO AND CORROSION OF METALS AT 70ºC / 168 HRS | BS 903: PART A 37 | MEETS REQUIREMENTS |
| POLYMER CONTENT (NITRILE) |  | 100% |
| ADDITIONAL INFORMATION - |  |  |
| CHEMICAL RESISTANCE |  |  |
| --- OZONE | BS 903: PART A 43 | FAIR |
| --- DILUTE ACIDS AND BASES | BS 903: PART A16 | GOOD |
| --- CONCENTRATED ACIDS AND BASES |  | NOT RECOMMENDED |
| --- MINERAL OIL/PETROLEUM |  | EXCELLENT |
| --- SOLVENTS |  | FAIR |
| TEMPERATURE RANGE |  | -30˚ to +120˚C |
| COLOUR | BLACK |  |
| VOLUME SWELL: AT 70 C FOR 72 HRS/IN | VALUES |  |
| IRM / ASTM OIL NO.1 | - 3 % |  |
| IRM / ASTM OIL NO.2 | - 2% |  |
| IRM / ASTM OIL NO.3 | + 10% |  |