Black Nitrile to BS2751 BA80 WJ193

| PROPERTIES | TEST METHOD | VALUES |
| --- | --- | --- |
|  |  | METRIC UNITS |
| DENSITY (Mg/m3) | BS 903: PART A1 | 1.25 ± 0.02 |
| HARDNESS | BS903: PART A26 | 80 (+5-4) IRHD |
| TENSILE STRENGTH (MIN) | BS 903: PART A2 | 12.5 Mpa |
| ELONGATION AT BREAK (MIN) | BS 903: PART A2 | 150% |
| COMPRESSION SET (70ºC/24 HRS/25% SET) (MAX) | BS 903: PART A6 | 20% |
| TEAR RESISTANCE (ANGULAR) MIN | BS 903: PART A3 | 55 Kg/cm |
| RESISTANCE TO ACCELERATED AGEING – 168 HRS AT 70˚C | BS 903: PART A19 |  |
| --- HARDNESS (Pts) | BS 903: PART A26 | + 10 (MAX) |
| --- TENSILE STRENGTH (%) | BS 903: PART A2 | -10 (MAX) |
| --- ELONGATION AT BREAK (%) | BS 903: PART A2 | -35 (MAX) |
| VOLUME SWELL: AT 40˚C FOR 24 HRS/IN | BS 903: PART A16 |  |
| FUEL B (MAX) |  | +25% |
| RESISTANCE TO LOW TEMPERATURE IN ºC AT WHICH THE STIFFNESS SHALL NOT EXCEED 70 MPA | BS 903: PART A13 | -15 |
| ADHESION TO AND CORROSION OF METALS AT 70ºC / 168 HRS | BS 903: PART A 37 | MEETS REQUIREMENTS |
| POLYMER CONTENT (NITRILE) |  | 100% |
| ADDITIONAL INFORMATION - |  |  |
| CHEMICAL RESISTANCE |  |  |
| --- OZONE | BS 903: PART A 43 | FAIR |
| --- DILUTE ACIDS AND BASES | BS 903: PART A16 | GOOD |
| --- CONCENTRATED ACIDS AND BASES |  | NOT RECOMMENDED |
| --- MINERAL OIL/PETROLEUM |  | EXCELLENT |
| --- SOLVENTS |  | FAIR |
| TEMPERATURE RANGE |  | -10˚ to +120˚C |
| COLOUR | BLACK |  |
| VOLUME SWELL: AT 70 C FOR 72 HRS/IN | VALUES |  |
| IRM / ASTM OIL NO.1 | - 3 % |  |
| IRM / ASTM OIL NO.2 | - 2% |  |
| IRM / ASTM OIL NO.3 | + 10% |  |

Failure to select the correct materials or products can result in damage to plant and equipment and personal injury. In specific applications, where critical conditions exist, we suggest you contact us, and we will consider with you the most suitable material or product. However, information supplied by William Johnston & Company Limited is intended only as technical co-operation and as a guide to the various uses of different products. No warranty is given in respect of information or recommendations by William Johnston & Company Limited which are only given for guidance and without any guarantee. The customer must satisfy themselves on the suitability of the material or product for the intended purpose. The correct fitting of products particularly is the responsibility of the customer.