Black Premium Grade NR SBR 40° shore WJ101

| PROPERTIES | TEST METHOD | VALUES FPS UNITS | TEST METHOD | VALUES METRIC UNITS |
| --- | --- | --- | --- | --- |
| SPECIFIC GRAVITY | DIN 53508 | 1.35±0.05 | ASTM D297 | 1.35±0.05 |
| HARDNESS | DIN 53505 | 40 ± 5 SH A | ASTM D2240 | 40 ± 5 SH A |
| TENSILE STRENGTH (MIN) | DIN 53504 | 713 PSI | ASTM D412 | 40 KG/CM2 |
| ELONGATION AT BREAK (MIN) | DIN 53504 | 250% | ASTM D412 | 250% |
| COMPRESSION SET (70ºC/24 HRS/25% COMPRESSION) (MAX) | DIN 53517 | 40% | ASTM D395 METHOD B | 40% |
| TEAR RESISTANCE (ANGULAR) MIN | DIN 53515 | 112 LBS/INCH | ASTM D624 | 20 KG/CM |
| CHANGE IN PROPERTIES AFTER |  |  |  |  |
| HEAT AGEING FOR (72 HRS. AT 70 ºC) |  |  | ASTM D573 |  |
| --- HARDNESS (PTS) |  | + 5 (MAX) |  | + 5 (MAX) |
| --- TENSILE STRENGTH (%) |  | + 10 / -25 |  | + 10 / -25 |
| --- ELONGATION AT BREAK (%) |  | + 10 / -25 |  | + 10 / -25 |
| VOLUME SWELL: AT 70ºC FOR 72 HRS |  |  | ASTM D 471 |  |
| IN IRM OIL NO.1 |  | NOT RECOMMENDED |  | NOT RECOMMENDED |
| IN IRM OIL NO.2 |  | NOT RECOMMENDED |  | NOT RECOMMENDED |
| IN IRM OIL NO.3 |  | NOT RECOMMENDED |  | NOT RECOMMENDED |
| CHEMICAL RESISTANCE |  |  |  |  |
| --- OZONE |  | NOT RECOMMENDED | ASTM D 1149 | NOT RECOMMENDED |
| --- DILUTE ACIDS AND BASES |  | NOT RECOMMENDED |  | NOT RECOMMENDED |
| --- CONCENTRATED ACIDS AND BASES |  | NOT RECOMMENDED |  | NOT RECOMMENDED |
| --- OILS |  | NOT RECOMMENDED |  | NOT RECOMMENDED |
| --- SOLVENTS |  | NOT RECOMMENDED |  | NOT RECOMMENDED |
| TEMPERATURE RANGE |  | -20º TO + 70 ºC |  | -20º TO + 70 ºC |
| COLOUR |  | BLACK |  |  |