Black Soft Commercial Quality Neoprene SBR Rubber 50° shore WJ132

| PROPERTIES | TEST METHOD | VALUES FPS UNITS | TEST METHOD | VALUES METRIC UNITS |
| --- | --- | --- | --- | --- |
| SPECIFIC GRAVITY | DIN 53508 | 1.45 ± 0.05 | ASTM D297 | 1.45 ± 0.05 |
| HARDNESS | DIN 53505 | 50 ± 5 SH A | ASTM D2240 | 50 ± 5 SH A |
| TENSILE STRENGTH (MIN) | DIN 53504 | 569 PSI | ASTM D412 | 40 KG/CM2 |
| ELONGATION AT BREAK (MIN) | DIN 53504 | 200% | ASTM D412 | 200% |
| COMPRESSION SET (70 ºC/24 HRS/25% SET) (MAX) | DIN ISO 815-1 | 40% | ASTM D395 METHOD B | 40% |
| TEAR RESISTANCE (ANGULAR) MIN | DIN 53515 | 100 LBS/INCH | ASTM D624 | 18 KG/CM |
| CHANGE IN PROPERTIES |  |  |  |  |
| HEAT AGEING (72 HRS. AT 70 ºC) |  |  | ASTM D573 |  |
| --- HARDNESS (PTS) |  | + 5 (MAX) |  | + 5 (MAX) |
| --- TENSILE STRENGTH (%) |  | + 10 / - 25 |  | + 10 / - 25 |
| --- ELONGATION AT BREAK (%) |  | + 10 / - 25 |  | + 10 / - 25 |
| VOLUME SWELL: AT 70º C FOR 72 HRS/IN |  |  | ASTM D 471 |  |
| IRM OIL NO.1 |  | + 33% |  | + 33% |
| IRM OIL NO.2 |  | + 47% |  | + 47% |
| IRM OIL NO.3 |  | + 90% |  | + 90% |
| POLYMER CONTENT (NEOPRENE) |  | 10% |  | 10% |
| CHEMICAL RESISTANCE |  |  |  |  |
| --- OZONE |  | FAIR | ASTM D 1149 | FAIR |
| --- DILUTE ACIDS AND BASES |  | FAIR |  | FAIR |
| --- CONCENTRATED ACIDS AND BASES |  | NOT RECOMMENDED |  | NOT RECOMMENDED |
| --- OILS |  | NOT RECOMMENDED |  | NOT RECOMMENDED |
| --- SOLVENTS |  | NOT RECOMMENDED |  | NOT RECOMMENDED |
| TEMPERATURE RANGE |  | -30 º TO +90º C |  | -30 º TO +90º C |
| COLOUR |  | BLACK |  |  |