Blue Food Quality Nitrile Rubber 60° shore WJ166

# Approved to: US FDA 21 CFR177,2600 – EU1935/2004 and USP Class V1 Compliant

| PROPERTIES | TEST METHOD | VALUES FPS UNITS | TEST METHOD | VALUES METRIC UNITS |
| --- | --- | --- | --- | --- |
| SPECIFIC GRAVITY | ASTM D297 | 1.4 +- 0.05 | DIN 53508 | 1.4 +- 0.05 |
| HARDNESS | ASTM D2240 | 60 ± 5 SH A | DIN 53505 | 60 ± 5 SH A |
| TENSILE STRENGTH (MIN) | ASTM D412 | 1140 PSI | DIN 53504 | 60 KG/CM2 |
| ELONGATION AT BREAK (MIN) | ASTM D412 | 350% | DIN 53504 | 350% |
| COMPRESSION SET (70 ºC/24 HRS/25% SET) (MAX) | ASTM D395 METHOD B | 40% | DIN 53517 | 40% |
| TEAR RESISTANCE (ANGULAR) MIN | ASTM D624 | 112 LBS/INCH | DIN 53515 | 20 KG/CM |
| CHANGE IN PROPERTIES |  |  |  |  |
| HEAT AGEING (72 HRS. AT 70 ºC) | ASTM D573 |  |  |  |
| --- HARDNESS (PTS) |  | + 4 (MAX) |  | + 4 (MAX) |
| --- TENSILE STRENGTH (%) |  | + 10 / - 15 |  | + 10 / - 15 |
| --- ELONGATION AT BREAK (%) |  | + 10 / - 20 |  | + 10 / - 20 |
| VOLUME SWELL: AT 70º C FOR 72 HRS/IN | ASTM D 471 |  |  |  |
| ASTM OIL NO.1 |  | + 3 % |  | + 3 % |
| ASTM OIL NO.2 |  | + 16% |  | + 16% |
| ASTM OIL NO.3 |  | + 20% |  | + 20% |
| POLYMER CONTENT (NITRILE) |  | 100% |  | 100% |
| CHEMICAL RESISTANCE |  |  |  |  |
| --- OZONE | ASTM D 1149 | FAIR |  | FAIR |
| --- DILUTE ACIDS AND BASES |  | GOOD |  | GOOD |
| --- CONCENTRATED ACIDS AND BASES |  | NOT RECOMMENDED |  | NOT RECOMMENDED |
| --- OILS |  | GOOD |  | GOOD |

| PROPERTIES | TEST METHOD | VALUES FPS UNITS | TEST METHOD | VALUES METRIC UNITS |
| --- | --- | --- | --- | --- |
| --- SOLVENTS |  | FAIR |  | FAIR |
| TEMPERATURE RANGE |  | -25º TO + 110º C |  | -25º TO + 110º C |
| COLOUR |  | RAL 5017 BLUE |  | RAL 5017 BLUE |
| POLYMER CONTENT (%) |  | 100 |  |  |

# Test Name – Determination of Amount of extractives

Method: With reference to US FDA 21 CFR 177.2 00

| Extractants | Test Condition | Amount of Extractives mg/inch² | Acceptable limit mg/inch² | Conclusion |
| --- | --- | --- | --- | --- |
|  |  | 1 |  |  |
| Distilled Water | 70 °C for 2 hours | 10 | 20 | Pass |
| n-Hexane | 70 °C for 2 hours | 100 | 175 | Pass |

Note:

1. mg/inch² denotes Milligram per square inch

2. °C denotes Degrees Celsius

Failure to select the correct materials or products can result in damage to plant and equipment and personal injury. In specific applications, where critical conditions exist, we suggest you contact us, and we will consider with you the most suitable material or product. However, information supplied by William Johnston & Company Limited is intended only as technical co-operation and as a guide to the various uses of different products. No warranty is given in respect of information or recommendations by William Johnston & Company Limited which are only given for guidance and without any guarantee. The customer must satisfy themselves on the suitability of the material or product for the intended purpose. The correct fitting of products particularly is the responsibility of the customer.