Off-White Natural Rubber to BS1154 Y40 WJ221

| PROPERTIES | TEST METHOD | VALUES FPS UNITS | TEST METHOD | VALUES METRIC UNITS |
| --- | --- | --- | --- | --- |
| SPECIFIC GRAVITY | BS 903: PART A1 |  |  | 1.1 |
| HARDNESS | BS 903: PART A26 |  |  | 40 ± 5 IRHD |
| TENSILE STRENGTH (KG/CM2) | BS 903: PART A2 |  |  | 190 |
| ELONGATION AT BREAK (MIN) | BS 903: PART A2 |  |  | 600% |
| COMPRESSION SET (70 ºC/24 HRS/25% SET) (MAX) | BS 903: PART A6 |  |  | 30% |
| TEAR RESISTANCE (ANGULAR) MIN | BS 903: PART A3 |  |  | 30 KG/CM |
| ABRASION RESISTANCE |  |  |  | 120 |
| CHANGE IN PROPERTIES |  |  |  |  |
| HEAT AGEING (168 HRS. AT 70ºC) | BS 903: PART A 19 |  |  |  |
| --- HARDNESS (PTS) | BS 903: PART A26 |  |  | + 5 / -5 (MAX) |
| --- TENSILE STRENGTH (%) | BS 903: PART A2 |  |  | -10 (MAX) |
| --- ELONGATION AT BREAK (%) | BS 903: PART A2 |  |  | -15(MAX) |
| POLYMER CONTENT (NATURAL RUBBER) |  |  |  | 100% |
| ADDITIONAL INFORMATION - |  |  |  |  |
| CHEMICAL RESISTANCE |  |  |  |  |
| --- OZONE | BS 903: PART A43 |  |  | NOT RECOMMENDED |
| --- DILUTE ACIDS AND BASES | BS 903: PART A16 |  |  | NOT RECOMMENDED |
| --- CONCENTRATED ACIDS AND BASES |  |  |  | NOT RECOMMENDED |
| --- OILS |  |  |  | NOT RECOMMENDED |
| --- SOLVENTS |  |  |  | NOT RECOMMENDED |
| TEMPERATURE RANGE |  |  |  | -20º TO + 70ºC |
| COLOUR |  | OFF WHITE |  |  |