Red Natural Rubber High Abrasion Grade 45° shore WJ1320

| PROPERTIES | TEST METHOD | VALUES FPS UNITS | TEST METHOD | VALUES METRIC UNITS |
| --- | --- | --- | --- | --- |
| SPECIFIC GRAVITY | DIN 53508 | 1.2 ±0.05 | ASTM D297 | 1.2 ±0.05 |
| HARDNESS | DIN 53505 | 45 ± 5 SH A | ASTM D2240 | 45 ± 5 SH A |
| TENSILE STRENGTH (MIN) | DIN 53504 | 1425 PSI | ASTM D412 | 100 KG/CM2 |
| ELONGATION AT BREAK (MIN) | DIN 53504 | 400% | ASTM D412 | 400% |
| ABRASION RESISTANCE (MAX) | DIN 53516 | 150 MM3 | ASTM D5963 | 150 MM3 |
| COMPRESSION SET (70ºC/24 HRS/25% COMPRESSION) (MAX) | DIN 53517 | 35% | ASTM D395 METHOD B | 35% |
| TEAR RESISTANCE (ANGULAR) MIN | DIN 53515 | 140 LBS/INCH | ASTM D624 | 25 KG/CM |
| CHANGE IN PROPERTIES AFTER |  |  |  |  |
| HEAT AGEING FOR (72 HRS. AT 70 ºC) |  |  | ASTM D573 |  |
| --- HARDNESS (PTS) |  | + 5 (MAX) |  | + 5 (MAX) |
| --- TENSILE STRENGTH (%) |  | + 10 / - 20 |  | + 10 / - 20 |
| --- ELONGATION AT BREAK (%) |  | + 10 / - 20 |  | + 10 / - 20 |
| VOLUME SWELL: AT 70ºC FOR 72 HRS |  |  | ASTM D 471 |  |
| IN IRM OIL NO.1 |  | NOT RECOMMENDED |  | NOT RECOMMENDED |
| IN IRM OIL NO.2 |  | NOT RECOMMENDED |  | NOT RECOMMENDED |
| IN IRM OIL NO.3 |  | NOT RECOMMENDED |  | NOT RECOMMENDED |
| CHEMICAL RESISTANCE |  |  |  |  |
| --- OZONE |  | FAIR | ASTM D 1149 | FAIR |
| --- DILUTE ACIDS AND BASES |  | FAIR |  | FAIR |
| --- CONCENTRATED ACIDS AND BASES |  | NOT RECOMMENDED |  | NOT RECOMMENDED |
| --- OILS |  | NOT RECOMMENDED |  | NOT RECOMMENDED |
| --- SOLVENTS |  | NOT RECOMMENDED |  | NOT RECOMMENDED |
| TEMPERATURE RANGE |  | -25º TO + 70º C |  | -25º TO + 70º C |

| PROPERTIES | TEST METHOD | VALUES FPS UNITS | TEST METHOD | VALUES METRIC UNITS |
| --- | --- | --- | --- | --- |
| COLOUR |  | RED |  |  |