Super Soft Red Natural Rubber 38° Shore WJ155

| PROPERTIES | TEST METHOD | VALUES FPS UNITS | TEST METHOD | VALUES METRIC UNITS |
| --- | --- | --- | --- | --- |
| SPECIFIC GRAVITY | DIN 53508 | 0.98+0.05 | ASTM D297 | 0.98+0.05 |
| HARDNESS | DIN 53505 | 38± 5 SH A | ASTM D2240 | 38± 5 SH A |
| TENSILE STRENGTH (MIN) | DIN 53504 | 3415 PSI | ASTM D412 | 240 KG/CM2 |
| ELONGATION AT BREAK (MIN) | DIN 53504 | 810% | ASTM D412 | 810% |
| ABRASION RESISTANCE (MAX) | DIN 53516 | 80 MM3 | ASTM D5963 | 80 MM3 |
| COMPRESSION SET (70°C/24HRS/25% COMPRESSION) (MAX) | DIN 53517 | 20% | ASTM D395 METHOD B | 20% |
| TEAR RESISTANCE (ANGULAR) MIN | DIN 53515 | 224 LBS/INCH | ASTM D624 | 40 KG/CM |
| RESILIENCE |  | 75% |  | 75% |
| CHANGE IN PROPERTIES AFTER |  |  |  |  |
| HEAT AGEING FOR (72 HRS. AT 70°C) |  |  | ASTM D573 |  |
| --- HARDNESS (PTS) |  | + 3 (MAX) |  | + 3 (MAX) |
| --- TENSILE STRENGTH (%) |  | +10 / -15 |  | +10 / -15 |
| --- ELONGATION AT BREAK (%) |  | +10 / -15 |  | +10 / -15 |
| VOLUME SWELL: AT 70°C FOR 72 HRS |  |  | ASTM D 471 |  |
| IN IRM OIL NO.1 |  | NOT RECOMMENDED |  | NOT RECOMMENDED |
| IN IRM OIL NO.2 |  | NOT RECOMMENDED |  | NOT RECOMMENDED |
| IN IRM OIL NO.3 |  | NOT RECOMMENDED |  | NOT RECOMMENDED |
| CHEMICAL RESISTANCE |  |  |  |  |
| --- OZONE |  | FAIR | ASTM D 1149 | FAIR |
| --- DILUTE ACIDS AND BASES |  | GOOD |  | GOOD |
| --- CONCENTRATED ACIDS AND BASES |  | NOT RECOMMENDED |  | NOT RECOMMENDED |
| --- OILS |  | NOT RECOMMENDED |  | NOT RECOMMENDED |
| --- SOLVENTS |  | NOT RECOMMENDED |  | NOT RECOMMENDED |

| PROPERTIES | TEST METHOD | VALUES FPS UNITS | TEST METHOD | VALUES METRIC UNITS |
| --- | --- | --- | --- | --- |
| TEMPERATURE RANGE |  | -30° TO + 70° C |  | -30° TO + 70° C |
| COLOR |  | RED |  |  |

Failure to select the correct materials or products can result in damage to plant and equipment and personal injury. In specific applications, where critical conditions exist, we suggest you contact us, and we will consider with you the most suitable material or product. However, information supplied by William Johnston & Company Limited is intended only as technical co-operation and as a guide to the various uses of different products. No warranty is given in respect of information or recommendations by William Johnston & Company Limited which are only given for guidance and without any guarantee. The customer must satisfy themselves on the suitability of the material or product for the intended purpose. The correct fitting of products particularly is the responsibility of the customer.