# Ultraload Fibre Reinforced Bearing Pads

# Ultraload Fibre Reinforced Load Bearing Pads are manufactured using recycled high- quality tyres resulting in an economical and environmentally friendly product. The fully vulcanised rubber has inclusion of majorly dispersed fibres creating a unique compound that exhibits outstanding strength and durability. Ultraload can withstand harsh conditions like exposure to ozone and low temperatures. This product is commonly used in construction applications, prestress concrete bridges, buildings, machinery and equipment foundations.

# USES

# Bearing pads have a range of applications and are commonly used as handrail bearing pads, lighting standard pad seats, vibration isolation railway tie pads and in bridge bearing masonry along with other applications. If you are unsure whether this product is right for you, feel free to give us a call to discuss your requirements with one of our many experts.

# MATERIAL COMPOSITION

# The material is reinforced with synthetic fibre during the construction process of the sheet, increasing internal strength considerably. This unique process adds enhanced levels of tensile and compression strength, durability, tear resistance, stiffness and superior weather and ozone resistance. This could not be achieved without the fibre reinforcement.

| Physical Properties | Test Method | Specification of METROLOAD Bearing Pads |  |
| --- | --- | --- | --- |
| Tensile Strength, Min | ASTM D412, Die C | MD: 5.2 Mpa | MD: 754 PSI |
| Tear Strength, Min | ASTM D624, Die B | MD: 26.4 kN/m | MD: 150 PI M |
|  |  | TD: 52.5 kN/m | TD: 300 PI |
| Elongation, %, Min | ASTM D412, Die C | MD:15 TD: 40 |  |
| Hardness, Shore A | ASTM D2240 | 80 ± 5 |  |
| Specific Gravity | ASTM D297 sec. 16.3 | N/A |  |
| Ozone Resistance | ASTM D518 “B” | Application Specific |  |
| Low Temperature Resistance | ASTM D2137 at -40oC | Pass |  |
| Coefficient of Friction | ASTM D1894 | >0.8 |  |
| PHYSICAL PROPERTIES (HEAT AGED) | TEST METHOD ASTM D573, 70H at 70oC |  |  |
| Tensile Strength, Change % Max | ASTM D412, Die C | ±25 |  |
| Elongation, Change %, Max | ASTM D412, Die C | ±25 |  |
| Hardness, Change Pts | Max. ASTM D2240 | ±10 |  |

LOAD DEFLECTION