White Food Quality NR / SBR 60° shore WJ136

Approved to: US FDA21 CFR177,2600 & EU1935/2004 and USP Class 1 V1 Compliant

| PROPERTIES | TEST METHOD | VALUES | TEST METHOD | VALUES |
| --- | --- | --- | --- | --- |
|  |  | FPS UNITS |  | METRIC UNITS |
| SPECIFIC GRAVITY | DIN 53508 | 1.5 ± 0.05 | ASTM D297 | 1.5 ± 0.05 |
| HARDNESS | DIN 53505 | 60 ± 5 SH A | ASTM D2240 | 60 ± 5 SH A |
| TENSILE STRENGTH (MIN) | DIN 53504 | 1140 PSI | ASTM D412 | 60 KG/CM2 |
| ELONGATION AT BREAK (MIN) | DIN 53504 | 200% | ASTM D412 | 200% |
| COMPRESSION SET (70ºC/24 HRS/25% COMPRESSION) (MAX) | DIN ISO 815-1 | 40% | ASTM D395 METHOD B | 40% |
| POLYMER CONTENT |  | NA |  | NA |
| TEAR RESISTANCE (ANGULAR) MIN | DIN 53515 | 112 LBS/INCH | ASTM D624 | 20 KG/CM |
| CHANGE IN PROPERTIES AFTER |  |  |  |  |
| HEAT AGEING FOR (72 HRS. AT 70 ºC) |  |  | ASTM D573 |  |
| --- HARDNESS (PTS) |  | + 5 (MAX) |  | + 5 (MAX) |
| --- TENSILE STRENGTH (%) |  | + 10 / 15 |  | + 10 / 15 |
| --- ELONGATION AT BREAK (%) |  | + 10 / 15 |  | + 10 / 15 |
| VOLUME SWELL: AT 70ºC FOR 72 HRS |  |  | ASTM D 471 |  |
| IN IRMOIL NO.1 |  | NOT RECOMMENDED |  | NOT RECOMMENDED |
| IN IRMOIL NO.2 |  | NOT RECOMMENDED |  | NOT RECOMMENDED |
| IN IRMOIL NO.3 |  | NOT RECOMMENDED |  | NOT RECOMMENDED |
| CHEMICAL RESISTANCE |  |  |  |  |
| --- OZONE |  | NOT RECOMMENDED | ASTM D 1149 | NOT RECOMMENDED |
| --- DILUTE ACIDS AND BASES |  | NOT RECOMMENDED |  | NOT RECOMMENDED |
| --- CONCENTRATED ACIDS AND BASES |  | NOT RECOMMENDED |  | NOT RECOMMENDED |
| --- OILS |  | NOT RECOMMENDED |  | NOT RECOMMENDED |
| --- SOLVENTS |  | NOT RECOMMENDED |  | NOT RECOMMENDED |
| TEMPERATURE RANGE |  | -30 º TO + 70ºC |  | -30 º TO + 70ºC |
| COLOUR |  | OFF-WHITE |  | OFF-WHITE |

| TEST RESULTS: MIGRATION DATA |  |  |  |  |
| --- | --- | --- | --- | --- |
| (TEST NO. 1-I) SENSORY VERIFICATION OF ODOUR/SMELL |  |  |  |  |
| (TEST NO. 1-I) SENSORY VERIFICATION OF ODOUR/SMELL TEST SPECIFICATION(S)/REGULATION(S): REGULATION (EC) NO. 1935/2004 & COUNCIL OF EUROPE RESOLUTION RESAP (2004) 4 ON RUBBER PRODUCTS INTENDED TO COME INTO CONTACT WITH FOODSTUFFS. TEST METHOD ADOPTED: DIN 10955:2004. SIMULANT(S) USED: DISTILLED WATER. TEST CONDITION(S): 100 0C OR REFLUX FOR 4 HOURS. |  |  |  |  |
| COMPONENT NO. | TEST PARAMETER | RESULT (GRADE) | COMPLIANCE REQUIREMENT/LIMIT MAX. | CONLUSION (PASS/FAIL) REFER REMARK 3 ON PAGE NO.2) |
| A | RATING | 0 | LESS THAN 2.5 | PASS |
| Note: (INTERMEDIATE GRADES ARE ALLOWED) 0 = NO PERCEPTIBLE DIFFERENCE IN ODOUR. 1 = JUST PERCEPTIBLE DIFFERENCE IN ODOUR (STILL DIFFICULT TO DEFINE). 2 = SLIGHT DIFFERENCE IN ODOUR. 3 = MARKED DIFFERENCE IN ODOUR 4 = STRONG DIFFERENCE IN ODOUR |  |  |  |  |

| (TEST NO. 1-II) SENSORY VERIFICATION OF TASTE |  |  |  |  |
| --- | --- | --- | --- | --- |
| TEST SPECIFICATION(S)/REGULATION(S): REGULATION (EC) NO. 1935/2004 & COUNCIL OF EUROPE RESOLUTION RESAP (2004) 4 ON RUBBER PRODUCTS INTENDED TO COME INTO CONTACT WITH FOODSTUFFS. TEST METHOD ADOPTED: DIN 10955:2004. SIMULANT(S) USED: DISTILLED WATER. TEST CONDITION(S): 100°C OR REFLUX FOR 4 HOURS. |  |  |  |  |
| COMPONENT NO. | TEST PARAMETERS | RESULT (GRADE) | COMPLIANCE REQUIREMENT/LIMIT MAX. | CONCLUSION (PASS/FAIL) (REFER REMARK 3 ON PAGE NO.2) |
| A | RATING | 0 | LESS THAN 2.5 | PASS |
| Note: (INTERMEDIATE GRADES ARE ALLOWED) 0 = NO PERCEPTIBLE DIFFERENCE IN TASTE. 1 = JUST PERCEPTIBLE DIFFERENCE IN TASTE (STILL DIFFICULT TO DEFINE). 2 = SLIGHT DIFFERENCE IN TASTE. 3 = MARKED DIFFERENCE IN TASTE. 4 = STRONG DIFFERENCE IN TASTE. |  |  |  |  |

| (TEST NO. 2) OVERALL MIGRATION |  |  |  |  |
| --- | --- | --- | --- | --- |
| TEST SPECIFICATION(S)/REGULATION(S): COUNCIL OF EUROPE RESOLUTION RESAP (2004) 4 ON RUBBER PRODUCTS INTENDED TO COME INTO CONTACT WITH FOODSTUFFS. TEST METHOD(S) ADOPTED: WITH REFERENCE TO EN 1186-3:2002 (FOR 3 % ACETIC ACID) & EN 1186-14:2002 (FOR 95 % ETHANOL AND ISO-OCTANE); SIMULANTS USED: REFER BELOW. TEST CONDITION(S): REFER BELOW (NOTE: TESTS CONDUCTED UNDER REPEAT-USE CONDITIONS); |  |  |  |  |
| S.NO. | SIMULANT USED | TEST CONDITION(S) | COMPONENT NO. | RESULT (MG/KG) |
| 1 | 3 % ACETIC ACID | 100 °C OR REFLUX FOR 4 HOURS | A | ND |
| 2 | 95 % ETHANOL | 60 °C FOR 6 HOURS | A | ND |
| 3 | ISO- OCTANE | 60 °C FOR 4 HOURS | A | ND |
| OVERALL CONCLUSION (PASS/FAIL) |  |  |  | Pass |
| LIMIT OF QUANTIFICATION: 12.0 MG/KG |  |  |  |  |
| Note (1) “MG/KG” DENOTES MILLIGRAM PER KILOGRAM: (2) °C DENOTES DEGREES CELCIUS. (3) “%” DENOTES PER CENT. (4) “ND” DENOTES NOT DETECTED |  |  |  |  |

| (TEST NO. 3) Specific migration of primary aromatic amines |  |  |  |  |
| --- | --- | --- | --- | --- |
| TEST SPECIFICATION(S)/REGULATION(S): COUNCIL OF EUROPE RESOLUTION RESAP (2004) 4 ON RUBBER PRODUCTS INTENDED TO COME INTO CONTACT WITH FOODSTUFFS. TEST METHOD(S) ADOPTED: WITH REFERENCE TO EN 13130-1:2004 FOLLOWED BY ANALYSIS USING UV VISIBLE SPECTROPHOTOMETER. SIMULANT(S) USED: 3 % ACETIC ACID. TEST CONDITION(S): 100 °C OR REFLUX FOR 4 HOURS (UNDER REPEAT-USE CONDITIONS); EQUIPMENT(S) USED: UV VISIBLE SPECTROPHOTOMETER. |  |  |  |  |
| COMPONENT NO. | RESULT (MG/KG) | LIMIT OF QUANTIFICATION (MG/KG) | COMPLIANCE REQUIREMENT/LIMIT MAX. | CONCLUSION (PASS/FAIL) |
| A | ND | 0.01 | SUM OF PRIMARY AROMATIC AMINES SHALL BE LESS THAN 0.01 MG/KG | PASS |
| Note: (1) “MG/KG” DENOTES MILLIGRAM PER KILOGRAM: (2) °C DENOTES DEGREES CELCIUS. (3) “%” DENOTES PER CENT. (4) “ND” DENOTES NOT DETECTED. (5) “UV” DENOTES ULTRA-VIOLET |  |  |  |  |

| (TEST NO. 4-I) SPECIFIC MIGRATION OF PHTHALATES |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| TEST SPECIFICATION(S)/REGULATION(S): COUNCIL OF EUROPE RESOLUTION RESAP (2004) 4 ON RUBBER PRODUCTS INTENDED TO COME INTO CONTACT WITH FOODSTUFF. TEST METHOD(S) ADOPTED: WITH REFERENCE TO EN 13130-1:2004 FOLLOWED BY ANALYSIS USING GC MS; SIMULANT(S) USED: 95 % ETHANOL. TEST CONDITION(S): 60 °C FOR 6 HOURS (UNDER REPEAT-USE CONDITIONS). EQUIPMENT(S) USED: GC MS (GAS CHROMATOGRAPHY MASS SPECTROMETER). |  |  |  |  |  |  |
| S.NO | PARAMETER | CAS NO. | RESULT (MG/KG) – COMPONENT NO. A | LIMIT OF QUANTIFICATION (MG/KG) | COMPLIANCE REQUIREMENT/LIMIT MAX. | CONCLUSION (PASS/FAIL) (REFER REMARK 3 ON PAGE NO.2) |
| 1 | BENZYLBUTYL PHTHALATE (BBP) | 85- 68-7 | ND | 0.3 | NOT TO EXCEED 6 MG/KG | PASS |
| 2 | DIETHYLHEXYL PHTHALATE (DEHP) | 117- 81-7 | ND | 0.3 | NOT TO EXCEED 3 MG/KG | PASS |
| 3 | DIBUTYL PHTHALATE (DBP) | 84- 74-2 | ND | 0.3 | NOT TO EXCEED 3 MG/KG | PASS |
| 4 | DICYCLOHEXYL PHTHALATE (DCHP) | 84- 61-7 | ND | 0.3 | NOT TO EXCEED 6 MG/KG | PASS |
| 5 | DIETHYL PHTHALATE (DEP) | 84- 66-2 | ND | 0.3 | NOT TO EXCEED 12 MG/KG | PASS |
| OVERALL CONCLUSION (PASS/FAIL) |  |  |  |  |  | PASS |
| Note (1) “MG/KG” DENOTES MILLIGRAM PER KILOGRAM: (2)”ND” DENOTES NOT DETECTED. (3) °C DENOTES DEGREES CELCIUS. (4) “%” DENOTES PERCENTAGE. |  |  |  |  |  |  |

| (Test No. 4-ii) Specific migration of phthalates |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Test Specification(s)/Regulation(s): Council of Europe Resolution ResAP (2004) 4 on rubber products intended to come into contact with foodstuff. Test method(s) adopted: With reference to EN 13130-1:2004 followed by analysis using GC MS; Simulant(s) used: Iso-octane. Test Condition(s): 60°C for 4 hours (under repeat-use conditions). Equipment(s) used: GC MS (Gas Chromatography Mass Spectrometer). |  |  |  |  |  |  |
| S. No. | Parameter | CAS No. | Result (mg/kg) - Component No. A | Limit of Quantification (mg/kg) | Compliance Requirement / Limit Max. | Conclusion (Pass/Fail) |
| 1 | Benzylbutyl phthalate (BBP) | 85-68-7 | ND | 0.3 | Not to exceed 6 mg/kg | Pass |
| 2 | Diethylhexyl phthalate (DEHP) | 117-81-7 | ND | 0.3 | Not to exceed 3 mg/kg | Pass |
| 3 | Dibutyl phthalate (DBP) | 84-74-2 | ND | 0.3 | Not to exceed 3 mg/kg | Pass |
| 4 | Dicyclohexyl phthalate (DCHP) | 84-61-7 | ND | 0.3 | Not to exceed 6 mg/kg | Pass |
| 5 | Diethyl phthalate (DEP) | 84-66-2 | ND | 0.3 | Not to exceed 12 mg/kg | Pass |
| Overall Conclusion (Pass/Fail) |  |  |  |  |  | Pass |
| Note: "mg/kg" denotes milligram per kilogram: (2) "ND" denotes Not Detected; (3) °C denotes degrees Celsius; (4) "%" denotes percentage. |  |  |  |  |  |  |

| (TEST NO. 5) Migration of N-Nitrosamines & N-Nitrosatable substances |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| TEST SPECIFICATION(S)/REGULATION(S): COUNCIL OF EUROPE RESOLUTION RESAP (2004) 4 ON RUBBER PRODUCTS INTENDED TO COME INTO CONTACT WITH FOODSTUFF. TEST METHOD ADOPTED: BASED ON BS EN 12868:1999. EQUIPMENT(S) USED: GAS CHROMATOGRAPHY MASS SPECTROMETER (GC MS). |  |  |  |  |  |
| TEST PARAMETER | COMPONENT NO. | TEST RESULT (MG/KG) | LIMIT OF QUANTIFICATION (MG/KG) | COMPLIANCE REQUIREMENT/LIMIT MAX. | CONCLUSION (PASS/FAIL) |
| MIGRATION OF N- NITROSAMINE S | A | ND | 0.01 | SHALL BE LESS THAN 0.01 MG/KG | PASS |
| MIGRATION OF N- NITROSATABLE SUBSTANCES | A | ND | 0.1 | SHALL BE LESS THAN 0.1 MG/KG | PASS |
| Note: (1) “ND” denotes NOT Detected. (2) mg/kg denotes Milligram per Kilogram |  |  |  |  |  |

| (TEST NO. 6) SPECIFIC MIGRATION OF BUTADIENE (1,3-BUTADIENE) (CAS NO. 106-99-0) |  |  |  |  |
| --- | --- | --- | --- | --- |
| TEST SPECIFICATION(S)/REGULATION(S): COUNCIL OF EUROPE RESOLUTION RESAP (2004) 4 ON RUBBER PRODUCTS INTENDED TO COME INTO CONTACT WITH FOODSTUFF; |  |  |  |  |
| TEST METHOD(S) ADOPTED: WITH REFERENCE TO EN 13130-1:2004 FOLLOWED BY ANALYSIS AS PER DD CEN/TS 13130- 15:2005; SIMULANTS USED: 3 % ACETIC ACID; TEST CONDITION(S): 100 °C OR REFLUX FOR 4 HOURS (UNDER REPEAT-USE CONDITIONS); EQUIPMENT(S) USED: GAS CHROMATOGRAPHY MASS SPECTROMETER (GC MS); |  |  |  |  |
| COMPONENT NO. | RESULT (MG/KG) | METHOD DETECTION LIMIT | COMPLIANCE REQUIREMENT/LIMIT MAX. | CONCLUSION (PASS/FAIL) |
| A | ND | 0.2 MG/KG | SHALL BE LESS THAN 0.02MG/KG | PASS |
| Note: (1) “MG/KG” DENOTES MILLIGRAM PER KILOGRAM: (2) °C DENOTES DEGRESS CELCIUS. (3) “%” DENOTES PERCENTAGE (4) DENOTES NOT DETECTED END OF TEST REPORT |  |  |  |  |