White Silicone Food Quality – 60° shore WJ14105

# FDA 21 CFR No: 177 – 2600 & EU1935/2004 regulations and USO Class V1 Compliant

| PROPERTIES | TEST METHOD | VALUES FPS UNITS | TEST METHOD | VALUES METRIC UNITS |
| --- | --- | --- | --- | --- |
| SPECIFIC GRAVITY | DIN 53508 | 1.20±0.05 | ASTM D297 | 1.20±0.05 |
| HARDNESS | DIN 53505 | 60 ± 5 | ASTM D2240 | 60 ± 5 |
| TENSILE STRENGTH (KG/CM2) | DIN 53504 | 712 PSI | ASTM D412 | 60 KG/CM2 |
| ELONGATION AT BREAK % (MIN) | DIN 53504 | 250 | ASTM D412 | 250 |
| COMPRESSION SET (150º C/24 HRS/25% SET) (MAX) | DIN ISO 815-1 | 40% | ASTM D395 METHOD B | 40% |
| TEAR RESISTANCE (ANGULAR) MIN | DIN 53515 | 112 LBS/INCH | ASTM D624 | 20 KG/CM |
| POLYMER CONTENT (%) |  | 100% |  | 100% |
| CHANGE IN PROPERTIES |  |  |  |  |
| HEAT AGEING (72 HRS. AT 100 ºC) |  |  | ASTM D573 |  |
| --- HARDNESS (PTS) |  | 3 |  | 3 |
| --- TENSILE STRENGTH (%) |  | ±5 |  | ±5 |
| --- ELONGATION AT BREAK (%) |  | ±5 |  | ±5 |
| WRAS QUALITY TEST |  | APPROVED | BS 6920: PART 3: 2000 | APPROVED |
| VOLUME SWELL: AT 70º C FOR 72 HRS/IN |  |  | ASTM D 471 |  |
| OZONE (20% STRETCH 40°C FOR 72 HRS AT 50 PPHM) |  | EXCELLENT | ASTM D 1149 | EXCELLENT |
| --- DILUTE ACIDS AND BASES |  | EXCELLENT |  | EXCELLENT |
| --- CONCENTRATED ACIDS AND BASES |  | EXCELLENT |  | EXCELLENT |
| TEMPERATURE RANGE |  | -50 to 200°C |  | -50 to 200°C |
| COLOUR |  | WHITE |  | WHITE |

| Sr. No. | Net Chloroform Soluble Extractives using | Result | Unit | Limits as per standard | Test Method |
| --- | --- | --- | --- | --- | --- |
| Total Extractives at Reflux Temperatures for 7 hrs. Using |  |  |  |  |  |
| 1 | Distilled Water | 2.8 | mg/inch2 | 20.0 | As per USFDA 21.CFR.176.2600 |
| 2 | n-Hexane | 22.4 |  | 175.0 |  |
| Total Extractives at Reflux Temperatures for 2 hrs. Using |  |  |  |  |  |
| 3 | Distilled water | 0.8 | mg/inch2 | 1.0 |  |
| 4 | n-Hexane | 0.8 |  | 4.0 |  |

Note: Detection Limit for the method is 0.5 mg/inch2.

Failure to select the correct materials or products can result in damage to plant and equipment and personal injury. In specific applications, where critical conditions exist, we suggest you contact us, and we will consider with you the most suitable material or product. However, information supplied by William Johnston & Company Limited is intended only as technical co-operation and as a guide to the various uses of different products. No warranty is given in respect of information or recommendations by William Johnston & Company Limited which are only given for guidance and without any guarantee. The customer must satisfy themselves on the suitability of the material or product for the intended purpose. The correct fitting of products particularly is the responsibility of the customer.