
[image: image1.png]uuuuuuuu




JINGDONG RUBBER CO., LTD.

Beihuan Road, Renqiu City, Hebei Province,China

Certificate of Conformity
Product Name (产品名称)：     
1） Neoprene rubber sheet
Content:  a minimum of 8% Neoprene content.
	SPECIFICATION: COMMERCIAL NEOPRENE (MIN 8%)

	 
	
	
	
	
	
	 

	 
	
	
	
	
	
	 

	Basic Properties
	
	Value
	
	Test Method
	
	Unit

	Base Polymer Type
	 
	SBR/CR
	 
	 
	 
	 

	Indentation Hardness
	
	65 Shore A  (-4/+5)
	
	ATSM D22400 00
	
	Degrees

	Specific Gravity
	 
	1.5 (+/- 0.05)
	 
	ASTM D792
	 
	g/cm3

	Tensile Strength (Min)
	
	3
	
	ASTM D412
	
	Mpa

	Elongation @ Break (Min)
	 
	250
	 
	ASTM D412
	 
	%

	Min Continuous Working Temp
	
	-20
	
	
	
	Deg C

	Max Continuous Working Temp
	 
	+70
	 
	 
	 
	Deg C

	Max Intermittent Working Temp
	
	+90
	
	
	
	Deg C

	Compression Set 70 Deg 22 Hrs
	 
	35% Max
	 
	ASTM D395 Method B
	 
	%


2）SBR rubber sheet
	SPECIFICATION: COMMERCIAL SBR

	 
	
	
	
	
	
	 

	 
	
	
	
	
	
	 

	Basic Properties
	
	Value
	
	Test Method
	
	Unit

	Base Polymer Type
	 
	NR/SBR
	 
	 
	 
	 

	Indentation Hardness
	
	65 Shore A  (-4/+5)
	
	ATSM D22400 00
	
	Degrees

	Specific Gravity
	 
	1.5 (+/- 0.05)
	 
	ASTM D792
	 
	g/cm3

	Tensile Strength (Min)
	
	3
	
	ASTM D412
	
	Mpa

	Elongation @ Break (Min)
	 
	250
	 
	ASTM D412
	 
	%

	Min Continuous Working Temp
	
	-30
	
	
	
	Deg C

	Max Continuous Working Temp
	 
	+70
	 
	 
	 
	Deg C

	Max Intermittent Working Temp
	
	+90
	
	
	
	Deg C

	Compression Set 70 Deg 22 Hrs
	 
	30% Max
	 
	ASTM D395 Method B
	 
	%

	
	
	
	
	
	
	


3) CVOMMERCIAL INSERTION
	SPECIFICATION: COMMERCIAL INSERTION

	 
	
	
	
	
	
	 

	 
	
	
	
	
	
	 

	Basic Properties
	
	Value
	
	Test Method
	
	Unit

	Base Polymer Type
	 
	NR/SBR
	 
	 
	 
	 

	Indentation Hardness
	
	65 Shore A  (-4/+5)
	
	ATSM D22400 00
	
	Degrees

	Specific Gravity
	 
	1.5 (+/- 0.05)
	 
	ASTM D792
	 
	g/cm3

	Tensile Strength (Min)
	
	3
	
	ASTM D412
	
	Mpa

	Elongation @ Break (Min)
	 
	250
	 
	ASTM D412
	 
	%

	Min Continuous Working Temp
	
	-30
	
	
	
	Deg C

	Max Continuous Working Temp
	 
	+70
	 
	 
	 
	Deg C

	Max Intermittent Working Temp
	
	+90
	
	
	
	Deg C

	Compression Set 70 Deg 22 Hrs
	 
	30% Max
	 
	ASTM D395 Method B
	 
	%

	Insertion Type
	 
	COTTON
	 
	 
	 
	 


Jingdong company hereby confirms that the submitted products of the Rubber product is under the specifications above mentioned.

Jingdong Rubber Co. ,Ltd
