[image: image1.png]TECHNICAL DATA SHEET FOR FIRE RETARDANT COMPOUND

SPECIAL PROPERTIES

MF775U CR

Stable over a range of temperatures 55 to +250c.
Fireretardant,low smoke emission, low toxic gas emission

PROPERTIES
| Shore hardness 6845

Tensile S.0MPa
Elongation @ break 0%
Tearstrength 15RNfm

Rebound resilience .

s A

HEAT STABILITY

Mechanical properties aftr heat azeing in hot air afer 10 days at 200c
[ Shore hardness il

Tensle strength 73MPa
Elongation 200%

Mechanical poperties aftr heat ageing i hot air afte 7 daysat 250c
[ Shore hardness kil

Temsle strength. 59MPa
Elongation 130
DIELECTRICAL PROPERTIES

‘Dicletric streagth(?mm) 2RV
Dilectric constant. 54 VEz

‘Elie tesistauce, opacicy and toxicicr of funes

Fire resstance-ULO4VO at 3mm, ULDA V1 af Jmm

Limit oxygen index.35% approx.
BS68S3 stats
Temperatue (FT) 341c
‘Smoke density (Ao max) 0.0162
Toxic fumes analysis 0.40





