

|  |  |
| --- | --- |
| **PRODUCT NAME** | **HYDROGENATED NITRILE 70** |
| **DESCRIPTION** | EXCELLENT RESISTANCE TO MINERAL OILS, LOW  |
|  | TEMPERATURE FLEXIBILITY, EXCELLENT  |
|  | RESISTANCE TO OZONE AND WEATHER GOOD  |
|  | RESISTANCE TO AGEING IN HOT AIR AND. |
|  | INDUSTRIAL LUBRICANTS, HOT WATER AND  |
|  | STEAM TO 150°C. RESISTANT TO AMINE BASED  |
|  | CORROSION INHIBITORS AND SOUR GAS (H2S), |
|  | RESISTANCE TO HIGH-ENERGY RADIATION |
| **THICKNESS (mm)** | 1.0, 2.0, 3.0, 5.0, 6.0, 8.0 |
| **SHEET SIZE** | 1.4M x 10M |
|  |  |
| **FINISH** | PLATE/PLATE |
| **MATERIAL** | HNBR |
| **APPLICATION** | AS ABOVE |
| **INSERTION** | NO |
| **CHEMICAL RESISTANCE** | PLEASE REFER TO OUR CHEMICAL DATA SHEET |

|  |  |
| --- | --- |
| **SPECIFICATIONS****COMPOUND** | Values(Typical) |
| **COLOUR** | BLACK |
| **COMPOUND** | HNBR |
| **DENSITY (SPECIFIC GRAVITY) g/cm³** | 1.40 |
| **HARDNESS (DEGREES SHORE A) +/-5** | 70 |
| **TENSILE STRENGTH MPa** | 11.0 |
| **ELONGATION AT BREAK %** | 400 |
| **MINIMUM TEMPERATURE ◦C** | -25 |
| **MAXIMUM TEMPERATURE ◦C** | +150 |
|  |  |

Failure to select the correct materials or products can result in damage to plant and equipment and personal injury. In specific applications, particularly where critical conditions exist, we suggest you contact us and we will consider with you the most suitable material or product. However, information supplied by William Johnston & Company Limited is intended only as technical co-operation and as a guide to the various uses of different products. No warranty is given in respect of information or recommendations by William Johnston & Company Limited which are only given for guidance and without any guarantee. The customer must satisfy themselves on the suitability of the material or product for the intended purpose. The correct fitting of products is the responsibility of the customer.