

|  |  |
| --- | --- |
| **PRODUCT NAME** | **NITRILE 70** |
| **DESCRIPTION** | BLACK NITRILE FUEL GRADE RUBBER SHEET  |
|  | THIS COMPOUND NITRILE RUBBER IS |
|  |  SUITABLE FOR N INSTANCES SUCH AS GASKETS |
|  | AND SEALS WHERE OIL BASED PRODUCTS |
|  | ARE PRESENT, FUEL RESISTANCE IS REQUIRED |
|  | OR FOR GENERAL PURPOSE USAGE. |
| **THICKNESS (mm)** | 1.0, 1.5, 2.0, 3.0, 4.0, 5.0, 6.0, 8.0, 10.0, 12.0 |
| **SHEET SIZE** | 1.4M X 5M, 1.4M X 10M |
|  |  |
| **FINISH** | PLATE/PLATE |
| **MATERIAL** | NBR |
| **APPLICATION** | GENERAL OIL RESISTANCE |
| **INSERTION** | NO |
| **CHEMICAL RESISTANCE** | PLEASE REFER TO OUR CHEMICAL DATA SHEET |

|  |  |
| --- | --- |
| **SPECIFICATIONS****COMPOUND** | Values(Typical) |
| **COLOUR** | BLACK |
| **COMPOUND** | NBR/SBR |
| **DENSITY (SPECIFIC GRAVITY) g/cm³** | 1.45 |
| **HARDNESS (DEGREES SHORE A) +/-5** | 70 |
| **TENSILE STRENGTH MPa** | 5.0 |
| **ELONGATION AT BREAK %** | 250 |
| **MINIMUM TEMPERATURE ◦C** | -20 |
| **MAXIMUM TEMPERATURE ◦C** | +90 |
|  |  |

Failure to select the correct materials or products can result in damage to plant and equipment and personal injury. In specific applications, particularly where critical conditions exist, we suggest you contact us and we will consider with you the most suitable material or product. However, information supplied by William Johnston & Company Limited is intended only as technical co-operation and as a guide to the various uses of different products. No warranty is given in respect of information or recommendations by William Johnston & Company Limited which are only given for guidance and without any guarantee. The customer must satisfy themselves on the suitability of the material or product for the intended purpose. The correct fitting of products is the responsibility of the customer.