TECHNICAL DATA

Inverness +44 (0) 1463 238 673 Head Office +44 (0) 141 620 1666 (8 lines) sales@williamjohnston.co.uk www.williamjohnston.co.uk

PRODUCT NAME	Viton
DESCRIPTION	Genuine Viton
THICKNESS (mm)	0.5mm to 10mm
SHEET SIZE (M)	1.2MX10M up to 6mm, 8mm & 10mm 1.2MX5M
FINISH	Plate
MATERIAL	Viton
APPLICATION	Outstanding resistance to chemicals, acids, oils and petroleum at high temperatures
INSERTION	no
CHEMICAL RESISTANCE	PLEASE REFER TO OUR CHEMICAL DATA SHEET
SPECIFICATIONS COMPOUND	Values [typical]
COLOUR	Black
COMPOUND	Viton (Dupont)
DENSITY [SPECIFIC GRAVITY] g/cm³	1.95
HARDNESS [DEGREES SHORE A] +/-5	70
TENSILE STRENGTH MPa	4.90
ELONGATION AT BREAK %	200
MINIMUM TEMPERATURE °C	-20
MAXIMUM TEMPERATURE °C	+300
COMPRESSION SET (70°C- 22 HRS) %	62

As the companies’ products are used in multiple applications and as the company has no control over the method of their use, the company excludes all conditions or warranties, expressed or implied by statute or otherwise. Any technical co-operation is given for customers’ assistance only and without liability on the part of the company.