EPDM WRc Approved

Product Description

EPDM elastomer, with good physical properties, excellent ageing and Ozone resistance,

which meets the requirements of BS 6920 W70, BS EN 681-1

Areas of Application

EPDM has been developed for uses as seals in areas where it will be in contact with cold

water.

It is not suitable in applications where it is likely to come into contact with hydrocarbons

(oils).

The WRC Listing Numbers are : 0907528 & 0808510

Physical Properties

| Property | Standard | Unit | Figure: |
| --- | --- | --- | --- |
| Density | BS 903 Part A1 | gms\cm³ | 1.22 +/- 0.03 |
| Hardness | BS 903 Part A26 | IRHD | 66 – 75 |
| Tensile Strength | BS 903 Part A2 | MPa | 9.0 Min |
| Elongation @ Break | BS 903 Part A2 | % | 200% Min |
| Compression Set | BS 903 Part A6 | % @ 23 C % @ 70 C | 15% Max 20% Max |
| Temperature Range ( continuous application) | Not Applicable | Degrees Centigrade | -15 to + 110 |
| Polymer Type | EPDM |  |  |
| Colour | Black |  |  |